Technical Specifications of Antistatic PU Foam

- Colour				:	Pink / Orange

- Thickness			:	10 mm

- Density			:	24 kg / mt3

- Surface Resistance		:	≤ 1011Ohms

- Static Charge Generation	:	≤ 200 Volts

- Rate of Decay			:	≤ 10 Sec

Technical Specifications of Antistatic – Conductive  PU Foam

- Colour				:	Black

- Thickness			:	10 mm

- Density			:	40 kg / mt3

- Surface Resistance		:	≤ 105Ohms

- Static Charge Generation	:	Nil

- Rate of Decay			:	≤ 2 Sec

Technical Specifications of Antistatic Stretch wrap film

- Colour				:	Transparent

- Thickness			:	23 +/- 2 µ

- Base Polymer			:	LLDPE

- Temp Resistance		:	650C

- Resistance to 			:	Water / Acid / Alkali

- Antistatic Properties

Surface Resistance		:	≤ 1011 Ohms / Sq cm

Rate of Decay			:	≤ 10 Sec

Static Charge Generation	:	≤ 200 Volts

Technical Specifications of VCI Film

- Colour				:	Transparent Yellow

- Thickness			:	23 +/- 2 µ

- Density			:	0.94 g/cc

- Base Material			:	LLDPE

- Corrosion Resistance		:	Steel

- Shelf life			:	2 Years